Exploring Machine Learning Models for Predicting Sheet Resistance of Laser‑Induced Graphene

Problem Statement

Laser-Induced Graphene (LIG) is a porous, three-dimensional graphene material formed by direct laser irradiation of carbon-rich polymer substrates; most commonly polyimide (PI). Its electrical conductivity/resistance is a critical functional property that determines its suitability for applications in flexible electronics, sensors, and energy storage devices. However, its sheet resistance depends sensitively on laser parameters such as Laser power, lasing speed, DPI, and defocus (10.1016/j.snb.2025.137466). These relationships are nonlinear, coupled, and often experiment‑specific.

The influences of non-linear parameter terms and interactions between key parameters on the graphitization process present challenges for rapid, resource-efficient optimization. Traditional trial-and-error experimentation is costly and time-consuming, and the large parameter space makes exhaustive empirical search impractical (10.1021/acsomega.1c00309).

This project addresses the following research question: Can machine learning models accurately predict the sheet resistance of LIG from laser processing parameters (power, speed, defocus, DPI), and which model architecture performs best for this task?

Background

LIG is produced by irradiating polyimide films with a CO₂ laser, which locally heats the polymer above its graphitization temperature, converting the sp³-hybridized carbon of the polymer into sp²-hybridized graphene without any chemical reagents or vacuum environments. The LIG process, serendipitously invented by Lin et al. in 2014 (10.1038/ncomms6714), involves irradiating precursor materials with a laser, transferring enough energy to carbonize the surface in such a way to form graphene. While it has been shown that many materials can be employed in this process, PI remains the most popular, owing to its low price, high accessibility, and flexibility { 10.1021/acs.jchemed.2c01237}.

The four laser parameters used as input features in this study each play a distinct physical role:

Laser Power controls the energy deposited per unit time. Higher power increases graphitization depth and degree of graphene ordering, but excessive power leads to ablation and substrate damage.

Scan Speed controls dwell time of the laser at any given point. Slower speeds increase energy input and pore size. Increasing number of passes and overlapping of laser spots led to increased LIG pore sizes, larger graphene scales, and reduced sheet resistance (10.1007/s42823-022-00447-2).

Defocus (or off-focus value) changes the effective laser spot size, controlling energy density per unit area. The influence of image resolution and off-focus value on the sheet resistance of LIG is explained by the superposition mechanism of laser scanning spots. (10.1007/s11431-021-1918-8)

DPI (dots per inch) determines scanning line spacing and thus lateral energy overlap between adjacent laser passes. By systematically varying the DPI, the laser energy per unit area (EPUA) is tuned to induce controlled morphological and structural evolution within the graphene framework, enabling a remarkable transition in surface wettability alongside a significant reduction in sheet resistance { 10.1021/acsaenm.5c01050}.

Together, these four parameters jointly determine the total laser fluence (energy per unit area) delivered to the substrate. The fluence of the laser during the scanning procedure is the critical parameter to control the formation of porous graphene, and a contour plot of the resistance of LIG in terms of scanning speed and DPI shows complex, nonlinear behavior. The nonlinear coupling between these parameters motivates the use of data-driven, machine-learning-based regression models.

Machine Learning for Regression in General

K-Nearest Neighbors (KNN): A non-parametric, instance-based learner that predicts by averaging the outputs of the k closest training points in feature space. It is simple, interpretable, and effective in low-dimensional, dense datasets, but sensitive to feature scaling.

Random Forest (RF): An ensemble of decision trees trained on bootstrapped samples with random feature subsets. Ensemble learning methods generally exhibit better performance than traditional single models in materials property prediction tasks, and random forests in particular balance accuracy with interpretability via feature importance scores.

Support Vector Regression (SVR): Uses kernel functions to map inputs into a high-dimensional feature space, fitting a maximum-margin hyperplane. It is effective in small, high-dimensional datasets and is robust to outliers.

Neural Networks (NN): Multilayer perceptrons learn hierarchical, nonlinear feature representations via backpropagation. They are highly flexible but require careful regularization and more data to avoid overfitting.

XGBoost: An optimized gradient boosting algorithm built on ensembles of decision trees. XGBoost reformulates the gradient boosting algorithm to provide stronger regularization and improved protection against overfitting, and has found diverse applications in chemistry and materials science.

CatBoost:  An advanced gradient‑boosting algorithm that builds decision‑tree ensembles with special techniques to reduce overfitting and handle categorical data automatically.

Prior Art: Machine Learning for Materials Property Prediction

The application of ML to materials property prediction has grown substantially over the last decade, with approaches spanning composition-based models to graph neural networks on crystal structures.

The Matbench benchmark suite tasks include predicting optical, thermal, electronic, thermodynamic, tensile, and elastic properties given a materials composition and/or crystal structure, and found that crystal graph methods appear to outperform traditional machine learning methods given approximately 10,000 or more data points. This is particularly relevant for LIG datasets, which tend to be small (hundreds of samples), making classical ML models like RF and XGBoost strong contenders. In the context of electronic property prediction specifically, gradient boosted decision trees and random forests are more effective in predicting bandgaps of 2D materials with an R² above 90%, while support vector regression and multi-layer perceptron show R² above 70%, demonstrating a clear performance hierarchy among common ML models on electronic materials data (10.1371/journal.pone.0255637).

Several studies have also applied ML directly to processing-property relationships in laser-fabricated materials. Bayesian optimization was used to optimize laser writing parameters for LIG electrodes, yielding a sheet resistance as low as approximately 6.75 Ω/sq, demonstrating that machine learning can efficiently navigate the laser parameter space to achieve highly conductive electrodes. Similarly, a multilayer perceptron neural network classifier was trained to predict whether laser parameters are adequate to produce a continuous and thus conductive LIG line, using a laser simulation model combined with machine learning to facilitate tuning of laser parameters (Johnson Glucose).

To address the high computational requirements of molecular dynamics simulations of LIG formation, machine learning models including LSTM networks, support vector regression (SVR), and multilayer perceptrons (MLP) were implemented to predict LIG surface characteristics (10.1038/s41598-025-15945-2). This directly motivates the multi-model comparison approach of the present project.

Your Approach

This project frames LIG sheet resistance prediction as a supervised regression problem. Six ML models are trained and compared on an experimental dataset of LIG samples fabricated across a systematically varied parameter space.

Input Features:

Laser power (W or % of maximum)

Scan speed (mm/s or cm/s)

Defocus distance (mm)

DPI (dots per inch / image resolution)

Target Variable:

Sheet resistance (Ω/sq), measured via four-point probe

Models Compared:

Neural Network (NN): fully connected MLP, tuned with dropout regularization

K-Nearest Neighbors (KNN): with cross-validated k selection

Random Forest (RF): 100–500 estimators, tuned max depth

Decision Tree (DT): as interpretable baseline

XGBoost: gradient boosted trees with learning rate and depth tuning

CatBoost: gradient boosted trees with native handling of categorical features

Workflow:

Feature importance analysis (from RF) is used to identify which laser parameter most strongly governs sheet resistance

Data is normalized (min-max or standard scaling) before training, which is critical for KNN and NN

Dataset is split into training/test sets (e.g., 80/20), with k-fold cross-validation used to evaluate generalization

Hyperparameters for each model are tuned via grid search or random search on the training fold

Models are evaluated using R² and RMSE on the held-out test set

Data Analysis Approach

Data Preparation

Loaded LIG dataset from Excel

Cleaned column names

Detecting and removing outliers

Automatically detected the target column (sheet resistance)

Split into training/testing sets (80/20):

Data Analysis and Model Evaluation Metrics

Finding relationships among input features and sheet resistance

R² (coefficient of determination): Overall variance explained

RMSE (root mean squared error): penalizes large errors.

Code Setup

#General Import Libraries

import pandas as pd

import numpy as np

from sklearn.model_selection import train_test_split

import matplotlib.pyplot as plt

from sklearn.metrics import r2_score, mean_squared_error

#Data Loading & Relation Analysis

import seaborn as sns

url = 'https://github.com/mta-phy/5820x/raw/main/HWs/LIG.xlsx'

Data = pd.read_excel(url)

Power = Data.iloc[:, 0].to_numpy();

Speed = Data.iloc[:, 1].to_numpy();

DPI = Data.iloc[:, 2].to_numpy();

Defocus = Data.iloc[:, 3].to_numpy();

Sheet_resistance= Data.iloc[:, 4].to_numpy();

print(Data.head(5))

# Pairplot

cols = ["Power (W)", "Speed (cm/s)", "DPI", "Defocus (inch)","Sheet Resistance (ohm)"]

sns.pairplot(Data[cols], diag_kind="kde", corner=True, hue="DPI")

plt.show()

#Correlation Matrix and Heatmap

plt.figure(figsize=(8,8))

feature_names=['Power','Speed','DPI','Defocus','Sheet Resistance']

# Create the heatmap

cor = np.corrcoef(Data.iloc[:, 0:5], rowvar=False)

im = plt.imshow(cor, vmin=-1, vmax=1, cmap='terrain')

plt.colorbar(im, label="Correlation coefficient")

for i in range(len(feature_names)):

for j in range(len(feature_names)):

text = plt.text(j, i, f"{cor[i, j]:.2f}",

ha="center", va="center", color="black",

fontweight='bold')

plt.xticks(range(len(feature_names)), feature_names, rotation=45)

plt.yticks(range(len(feature_names)), feature_names)

plt.title("Correlation Matrix with Values")

plt.tight_layout()

plt.show()

# % Contributions of Input Parameters

from sklearn.ensemble import RandomForestRegressor

X = Data[["Power (W)", "Speed (cm/s)", "DPI", "Defocus (inch)"]]

y = Data["Sheet Resistance (ohm)"]

rf = RandomForestRegressor(n_estimators=500, random_state=0)

rf.fit(X, y)

labels = X.columns

sizes = rf.feature_importances_

plt.figure(figsize=(7,7))

plt.pie(sizes, labels=labels, autopct="%1.1f%%", startangle=140, colors=["#AB0000", "#323BFA", "#AAB000", "#23C1DE"])

plt.title("Feature Importance for Predicting Sheet Resistance")

plt.tight_layout()

plt.show()

#Data Splitting

df = pd.read_excel(url)

df.columns = df.columns.str.strip()

# Features (inputs) and target (output)

X = df[['Power (W)', 'Speed (cm/s)', 'DPI', 'Defocus (inch)']]

y = df['Sheet Resistance (ohm)']

X_train, X_test, y_train, y_test = train_test_split(X, y, test_size=0.2, random_state=42)

#ML Models

#Random Forest (RF)

from sklearn.ensemble import RandomForestRegressor

model = RandomForestRegressor(n_estimators=400,  random_state=42)

#Decision Tree (DT)

from sklearn.tree import DecisionTreeRegressor

model = DecisionTreeRegressor(random_state=42,  max_depth=5,  min_samples_leaf=3)

#K-Nearest Neighbors (KNN)

from sklearn.preprocessing import StandardScaler

from sklearn.neighbors import KNeighborsRegressor

# SCALING

scaler = StandardScaler()

X_train = scaler.fit_transform(X_train)

X_test = scaler.transform(X_test)

# KNN MODEL

model = KNeighborsRegressor(n_neighbors=4,  weights='distance' )

# Neural Network

from sklearn.preprocessing import StandardScaler

from sklearn.neural_network import MLPRegressor

from sklearn.pipeline import Pipeline

model = Pipeline([

("scaler_X", StandardScaler()),

("mlp", MLPRegressor(hidden_layer_sizes=(16, 8),  activation='relu',  solver='adam', alpha=0.01,

learning_rate_init=0.0005,   max_iter=5000,   early_stopping=True,  n_iter_no_change=50,  random_state=42 ))

])

# XGBoost

import xgboost as xgb

model = xgb.XGBRegressor (n_estimators=800, learning_rate=0.05, max_depth=5, subsample=0.8,  colsample_bytree=0.8,  random_state=42)

# CatBoost

from catboost import CatBoostRegressor

model = CatBoostRegressor(iterations=1000, depth=5,  learning_rate=0.03,  loss_function='RMSE',  random_seed=42, verbose=False)

Fitting and Training

model.fit(X_train, y_train)

# Predictions

y_train_pred = model.predict(X_train)

y_test_pred = model.predict(X_test)

# Metrics

train_r2 = r2_score(y_train, y_train_pred)

test_r2 = r2_score(y_test, y_test_pred)

train_rmse = np.sqrt(mean_squared_error(y_train, y_train_pred))

test_rmse = np.sqrt(mean_squared_error(y_test, y_test_pred))

Plotting of Each Model

plt.figure(figsize=(8, 8))

# Scatter points

plt.scatter(y_train, y_train_pred, color='blue', label='Train', alpha=0.7)

plt.scatter(y_test, y_test_pred, color='red', label='Test', alpha=0.7)

# Ideal line (y = x)

min_val = min(y.min(), y_train_pred.min(), y_test_pred.min())

max_val = max(y.max(), y_train_pred.max(), y_test_pred.max())

plt.plot([min_val, max_val], [min_val, max_val], 'k--', label='Ideal')

# Fit regression lines

train_fit = np.polyfit(y_train, y_train_pred, 1)

test_fit = np.polyfit(y_test, y_test_pred, 1)

plt.plot([min_val, max_val],

np.polyval(train_fit, [min_val, max_val]),

color='blue', linestyle='-')

plt.plot([min_val, max_val],

np.polyval(test_fit, [min_val, max_val]),

color='red', linestyle='-')

# Labels

plt.xlabel("Actual Sheet Resistance")

plt.ylabel("Predicted Sheet Resistance")

# Text box for metrics

plt.text(min_val + 10, max_val - 60,

f"Train R² = {train_r2:.3f}\nTest R² = {test_r2:.3f}",

bbox=dict(facecolor='white'))

plt.text(max_val - 120, min_val + 30,

f"Train RMSE = {train_rmse:.3f}\nTest RMSE = {test_rmse:.3f}",

bbox=dict(facecolor='white'))

plt.legend()

plt.grid(True)

plt.tight_layout()

plt.show()

Results

|  | Power (W) | Speed (cm/s) | DPI | Defocus (inch) | Sheet Resistance (ohm) |
| --- | --- | --- | --- | --- | --- |
| 0 | 58 | 19 | 400 | -0.1 | 7.1757 |
| 1 | 60 | 18 | 200 | 0.2 | 7.1757 |
| 2 | 50 | 17 | 600 | -0.1 | 8.8641 |
| 3 | 56 | 18 | 300 | -0.1 | 10.9746 |
| 4 | 55 | 16 | 400 | -0.2 | 11.3967 |