LIG in Sensing Application

|  | Laser-induced self-N-doped porous graphene as an electrochemical biosensor for femtomolar miRNA detection Laser reduction of commercial polyimide (PI) resulted in nitrogen-doped porous graphene. Self-N-doping increased conductivity and improved affinity with nucleic acids. Response to miRNA concentrations as low as 10 fM. Characterizations: SEM, EDX, Raman, XPS, electrochemical measurement |
| --- | --- |
|  | Bio-Graphene Sensors for Monitoring Moisture Levels in Wood and Ambient Environment The LIG sensor was fabricated directly on the commercial wooden blocks. Measure both the surrounding humidity level and the moisture content inside the wood. Sensors could be connected to a sensor readout system for remotely reading. The sensitivity of sensors fabricated on spruce and pine wood is 2.6 and 0.74 MΩ per % RH. Characterization: 4 Probe method, potentiostat for impedance, Controlled Climate Chamber, SEM, Raman, TGA |
|  | High-performance flexible humidity sensors for breath detection and non-touch switches LIG electrode is prepared on a polyimide film. GO was dropped on the above graphene electrode and then heated. The flexible humidity sensor, under different humidity levels, shows fast response and recovery times (2 - 35 seconds). Also verified for monitoring different respiratory rates, cough and rhinitis humidty. Characterization: SEM, EDX, Raman, IR. |
|  | Ultrasensitive Electrochemical Methane Sensors Based on Solid Polymer Electrolyte-Infused Laser-Induced Graphene Pd nanoparticles were prepared and then introduced on porous LIG electrodes via a simple solvent exchange approach. After 10 to 20 minutes of use, pores were blocked by the formation of liquid water; air drying after saturation enabled the device to regain >99%. Characterization: SEM, Raman, electrochemical analysis, CV, and potentiostatic measurements, FTIR |